Savannah Tank & Equipment Corp

Liquid Penetrant Examination

Color Contrast

Solvent Removable Penetrant Process

Procedure: PT-100

Rev: 0

This procedure has been reviewed and meets the requirements of ASME Section V, 2017 Edition and Section VIII Appendix 8

Reviewed and accepted by:

QC Manager: _____________________________	Date: _______________

Demonstration of Procedure PT-100:

Job No: _______________________	PT Examiner: ______________________________

Demonstration accepted by:

Authorized Inspector: ________________________	Date: ______________

- General

  - The evaluation of indications and acceptance standards on this procedure is in accordance with ASME Section VIII Division 1, ASME Section I, and ASME B31.1.

  - The liquid penetrant examination method is an effective means for detecting discontinuities in welds and base metals which are open to the surface.

  - Typical discontinuities detectable by this method are cracks, seams, laps, cold shuts, laminations, overlap, and porosity. This procedure covers flat and rounded surfaces or welds.

  - Personnel using this procedure for ASME Code work will be qualified and certified by the Company using Written Practice Procedure PTQUAL-1.

- References

- ASME Section VIII Div. 1, Pressure Vessels

- ASME Section I, Power Boilers

- ASME B31.1, Power Piping

- ASME Section V, Nondestructive Testing.

- Quality Control Manual

- National Board Inspection Code

- Penetrant Materials

  - This procedure permits the use of the penetrants, cleaners/removes and developers by Manufacturer as listed below. The penetrant, cleaner/remover, and developer must be from the same manufacturer.

| MANUFACTURER | PENETRANT | DEVELOPER | CLEANER/REMOVER |
| --- | --- | --- | --- |
| Magnaflux Corp. | SKL-SP1 OR SKL-SP2 | SKD-S2 | SKC-S |
| Met-L-Chek Co. | VP-31 | D-70 | E-99 |
| Sherwin Inc. | DP40 | D100 | DR60 |
| Dyna Flux Corp | P-HF | D-F | C-F |

  - Intermixing of penetrant materials from difference families or different manufacturers are not permitted.

- Precautions:

  - Use in a well-ventilated area

  - Avoid breathing vapor or spray mist

  - Avoid prolonged or repeated contact with skin

  - Avoid contact with eyes

  - See MSDS for further information

- Control of Contaminants:

  - Certification of contaminant content for all liquid penetrant materials used on nickel base alloys, austenitic stainless steel and titanium.  This certification shall include the penetrant manufacturers’ batch number and the test results obtained in accordance with ASME Section  V, Mandatory Appendix II of Article 6.

  - When examining nickel base alloys, all materials shall be analyzed individually for sulfur.  The total amount of sulfur shall not exceed 1% by weight.

  - When examining austenitic stainless steel or titanium, all materials shall be analyzed individually for chlorine and fluorine content.  The total amount of chlorine and fluorine shall not exceed 1% by weight.

- Procedure

  - The temperature of penetrant and the surface of the part being examined shall not be below 40° F nor above 125° F during complete procedure.

  - Surface Preparation and Pre-Cleaning

    - The surface of the part may be in the as-welded, as-rolled, as-cast, or as forged condition.

    - Surface preparation by grinding, machining, or other methods may be necessary where surface irregularities could mask indications.

    - Clean area to examined with Cleaner / Remover. The surface to be examined and all adjacent areas within 1” shall be free of all dirt, grease, lint, scale, welding flux, weld spatter, paint, oil, and other extraneous matter that could interfere with the examination.

    - Allow at least 5 minutes for surface to dry by evaporation or forced air prior to applying penetrant.

  - Penetrant Application & Dwell Time

    - Apply penetrant by dipping, brushing, or spraying.

    - If penetrant is applied by spraying using compressed air type apparatus, filters shall be placed on the upstream side near the air inlet to preclude contamination of the penetrant by oil, water, dirt, or sediment that may have collected in the lines.

    - For temperature range of 50 F to 125 F, allow a minimum penetration (dwell) time of 5 minutes with the exception of wrought materials being 10 minutes. For temperature range of 40 F to 50 F, the penetrant dwell time shall remain on the surge for a minimum of 10 minutes with wrought materials being 20 minutes..

    - Maximum dwell time is 2 hours and penetrant shall not be allowed to dry on the part.

  - Excess Penetrant Removal

    - Remove excess penetrant by wiping surface clean with a clean, dry, lint-free cloth or absorbent paper towel until most traces of the penetrant has been removed.

    - Remove remaining traces of penetrant by wiping with a cloth or absorbent paper towel lightly moistened with cleaner / remover.

    - Do not flush surface with cleaner / remover.

    - Allow at least 3 minutes but not more than 10 minutes for surface to dry by evaporation, blotting, wiping, or forced air prior to applying developer.

  - Application of Developer

    - The developer shall be applied using a wet developer application.

    - Shake developer can thoroughly until agitator rattles.

    - Apply developer as soon as possible but not more than 10 minutes after the excess penetrant has been removed. Aqueous developer may be applied to a wet or dry surface by dipping, brushing, spraying or other means provided a thin coating is obtained over the entire surface being examined.  Drying may be through normal evaporation or using warm air.  The use of warm air shall not raise the temperature of the part above 125oF.  Blotting is not permitted.

  - Interpretation

    - Final interpretation shall be made within 10 – 60 minutes after the wet developer coating is dry.

    - If discontinuities are difficult to evaluate because the penetrant diffuses excessively into the developer, closely observe the formation of indications during application of the developer. This may assist in characterizing and determining the extent of indications.

    - The developer should form a reasonably uniform white coating. Surface discontinuities are indicated by bleed-out of the penetrant which is normally a deep red color that stains the developer.

    - Indications with a light pink color may indicate excessive cleaning.

    - Inadequate cleaning may leave an excessive background making interpretation difficult.

    - A minimum light intensity of 100 foot-candles (fc) is required on the surface to be examined to ensure adequate sensitivity during examination and evaluation of indications.

- Evaluation

  - An indication of an imperfection may be larger than the imperfection that causes it; however, the size of the indication is the basis for acceptance evaluation. Only indications with major dimensions over 1/16” are considered relevant.

  - A linear indication is one having a length greater than three times the width.

  - A rounded indication is one of circular or elliptical shape with the length equal to or less than three times the width.

  - Questionable indications are reexamined to determine whether they are relevant.

- Acceptance Standards

  - All surfaces to be examined shall be free of:

    - Relevant linear indications

    - Relevant rounded indications greater than 3/16”

    - Four or more relevant rounded indications in a line separated by 1/16” or less (edge to edge)

    - In addition, for ASME B31.1; Ten or more rounded indications in any 6” of surface with the major dimension of this area not to exceed 6”

- Repair Requirements

  - Unacceptable imperfections will be repaired and reexamined.

  - When an imperfection is repaired by grinding or machining and does not require weld repair, the area will be blended into the surrounding surface to avoid sharp notches, crevices, and corners. The area will then be reexamined.

  - When an imperfection requires weld repair, the defect will be removed by grinding or machining and that area will be examined to verify that the defect has been removed. The area will be cleaned and welded. Then the area will be blended into the surrounding surface to avoid sharp notches, crevices, and corners. The area will then be reexamined.

    - Welding is performed using a qualified welding procedure and welder.

  - Nonrelevant indications will be verified to be nonrelevant by grinding, visual inspection, or reexamination with this procedure.

- Examination Records

  - The results of examination are recorded on the form titled “Liquid Penetrant Certification”.

    - The results will include a description of nonrejectable indications.

    - The results will include a description of rejectable indications.

    - The results include a description of repairs.

    - The results include a statement as to whether not the results are acceptable.

- Post-Examination Cleaning

  - Post-examination cleaning will be done after final evaluation and recording the results to remove developer and penetrant from the part using rags and cleaner / remover.

- Light Level Verification and Demonstration

This procedure has been demonstrated and is certified to meet the requirements of Section V, paragraph T-150.

Light Source: _______________________________

Technique: _________________________________

Light level verified to be __________ foot candles (minimum 100)

Verified by: ______________________________	Date: ____________

PT Examiner (signature)

Approved by: ____________________________		Date: ____________

Quality Control Manager (signature)

Accepted by: _____________________________	Date: ____________

Authorized Inspector

| REQUIREMENT | COMMENTS | ESSENTIAL | NONESSENTIAL |
| --- | --- | --- | --- |
| Identification of and any change in type or family group of penetrant materials including developers, emulsifiers, etc. | Para 3.1 | x |  |
| Surface Preparation (finishing and cleaning, including type of cleaning solvent) | Para 6.2 | x |  |
| Method of applying penetrant | Para 6.3 | x |  |
| Method of removing excess surface penetrant | Para 6.4 | x |  |
| Hydrophilic or lipophilic emulsifier concentration and dwell time in dip tanks and agitation time for hydrophilic emulsifiers | NA – This procedure is for solvent removable only | x |  |
| Hydrophilic emulsifier concentration in spray applications | NA – This procedure is for solvent removable only | x |  |
| Method of applying developer | Para 6.5 | x |  |
| Minimum and maximum time periods between steps and drying aids | Para(s) 6.2.4, 6.3.3, 6.3.4, 6.4.4, 6.5.3, and 6.6.1 | x |  |
| Decrease in penetrant dwell time | Para 6.3.3 | x |  |
| Increase in developer dwell time (Interpretation Time) | Para 6.5.3 | x |  |
| Minimum light intensity | Para 6.6.6 | x |  |
| Surface temperature outside 40 deg F to 125 deg F or as previously qualified | Para 6.1 | x |  |
| Performance demonstration, when required | Para 12.0 | x |  |
| Personnel qualification requirements | Para 1.4 |  | x |
| Materials, shapes, or sizes to be examined and the extent of examination | Para 1.3 |  | x |
| Post-examination cleaning technique | Para 11.1 |  | x |

LIQUID PENETRANT CERTIFICATION

This will certify that the welds described below were inspected by Liquid Penetrant Examination method in accordance with the requirements of the code or standard indicated below.

ASME Section VIII, Div. 1

ASME Section I

ASME Section B31.1

NBIC and/or Other Standard

Penetrant Manufacturer  				  Batch No. 		 Type

Remover Manufacturer  				  Batch No. 		 Type

Developer Manufacturer  				  Batch No. 		 Type

Visible or Fluorescent			Temperature during examination 		oF.

(circle one)

Material Examined 							Thickness

Lighting Equipment Used

WELD DESCRIPTION/LOCATION	INSPECTION RESULT

PT EXAMINER

PT EXAMINER SIGNATURE

WITNESSED BY

DATE 	 TIME

JOB NUMBER

CUSTOMER