NONCONFORMANCE REPORT

| NCR No. | 001-26 |  |  |  |  |  |  | DATE: | 1/7/2026 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| JOB No. | 089-25 |  |  |  |  |  |  | OTHER: |  |  |  |  |
| ITEM DESCRIPTION: |  |  |  |  | Roof Seam Field Weld Double Beveled |  |  |  |  |  |  |  |
| DESCRIPTION OF NONCONFORMANCE: |  |  |  |  |  |  |  |  |  |  |  |  |
| During shop visit it was noticed that the field weld edges of the roof plate were double beveled. The design drawing showed the field weld joint to be a single bevel configuration. Savannah Tank Drawing 089-25-3 Rev.1 (See Details) |  |  |  |  |  |  |  |  |  |  |  |  |
| QC INSPECTOR: |  |  |  |  |  |  |  |  |  |  |  |  |
| RECOMMENDED DISPOSITION |  |  |  |  |  |  |  |  |  |  |  |  |
| ☐ USE-AS-IS |  |  |  | ☒ REPAIR |  |  | ☐ RETURN TO VENDOR |  |  | ☐ OTHER |  |  |
| The incorrect bevel areas shall be removed to result in a square joint type. A backing bar will be added to the ship loose items to be used during field construction. Ship loose backing bar details – 4 Pieces, 1/8” X 6” X 12’ (304SS) |  |  |  |  |  |  |  |  |  |  |  |  |
| QC INSPECTOR: |  |  |  |  |  |  |  |  |  |  | DATE: |  |
| DISPOSITION APPROVAL/ACCEPTANCE |  |  |  |  |  |  |  |  |  |  |  |  |
| ENGINEERING APPROVAL:(IF REQUIRED) |  |  |  |  |  |  |  |  |  |  | DATE: |  |
| QUALITY CONTROL MGR APPROVAL: |  |  |  |  |  |  |  |  |  |  | DATE: |  |
| INSPECTOR ACCEPTANCE: |  |  |  |  |  | N/A |  |  |  |  | DATE: | N/A |
| DISPOSITION COMPLETED |  |  |  |  |  |  |  |  |  |  |  |  |
| COMPLETED DISPOSITION AS RECOMMENDED? Yes ☒ No ☐ COMMENTS: |  |  |  |  |  |  |  |  |  |  |  |  |
| QUALITY CONTROL MGR APPROVAL: |  |  |  |  |  |  |  |  |  |  | DATE: |  |
| INSPECTOR ACCEPTANCE: |  |  |  |  |  | N/A |  |  |  |  | DATE: | N/A |